Lecture-1

- Lecture-2

- Lecture-3

- Lecture-4

- Lecture-5

- Lecture-6

- Lecture-7

- Lecture-8

- Lecture-9

- Lecture-10

- Lecture-11

- Lecture-12

- Lecture-13

- Lecture-14

- Lecture-15

- Lecture-16

- Lecture-17

- Lecture-18

- Lecture-19

- Lecture-20

- Lecture-21

- Lecture-22

- Lecture-23

- Lecture-24

- Lecture-25

- Lecture-26

- Lecture-27

- Lecture-28

Lecture-2

### METAL CASTING PROCESSES

Casting is the process of forming objects by pouring liquid or viscous material into a prepared mold or form.

Examples: Carburetors, frying pans, engine blocks, crankshafts, railroad-car wheels, plumbing fixture, power tools, gun barrels, machine tool is bases etc.

Properly designed and properly produced casting do not have directional properties. Casting can produce complex shapes. Cast iron has also very good dampening characteristics.

## Importance of casting

Complex shapes can be produced.

Minimal directional properties are obtained

Hollow sections can be produced

Very large part can be produced.

Metals that are very difficult to machine can be used to produce an object.

## Metals that can be casted

Iron, steel, Al, brass, bronze, Magnesium and certain Zinc alloys.

Various Casting processes have been developed; each has its own characteristics and applications to meets specific engineering and service requirements.

Sand casting,

Die Casting,

Centrifugal Casting,

Shell-Mold Casting,

Investment Casting,

Permanent-Mold Casting etc.

###### Current trends

Continuing mechanization and automation of the casting process

Increasing demand for high-quality casting with close tolerances

There are two major categories of casting

Expendable mold casting

Permanent mold casting

Expendable molds:  Made of sand, plaster, ceramics and similar materials which are generally mixed with various binders or bonding agents, the molds are broken up to remove the casting.

Made of sand, plaster, ceramics and similar materials which are generally mixed with various binders or bonding agents, the molds are broken up to remove the casting.

Permanent molds: Used repeatedly and are designed in such a way that casting can be easily removed and the mold used for the next casting.

Composite Molds: Made of two or more different materials (such as sand, graphite, and metal) combining the advantages of each material. Used to improve mold strength, cooling rates and overall economics of the process.

## Sand Casting

A traditional method (has been used for millennia)

Steps consists of:

Placing a pattern in sand to make an imprint,

Incorporating a gating system,

Filling the resulting cavity with molten metal

Allowing the metal to cool until it solidifies

Breaking the sand mold and removing the casting.

Outline of production steps in a typical sand casting operation is shown in Figure:

Figure:

Although the origins of sand casting date back to ancient times, it is still the most prevalent form of casting.

Typical parts – M/C tool bases, engine blocks, cylinder heads, and pump housings.

## Sands

Most sand casting operations use silica sand (SiO2).

Inexpensive and suitable as mold material because of its resistance to high temperatures

Two general types of sands: Naturally bonded (bank sands) and synthetic (lake sands).

Synthetic sand is preferred (because its composition can be controlled more accurately).

Important factors in selecting sand for molds:

Sand having fine, round grains can be closely packed and forms a smooth mold surface. Good permeability of molds and cores allows gases and steam evolved escape easily. The mold should have good collapsibility to avoid defects in the casting such as (hot tearing and cracking).

So, selection of sand involves certain tradeoffs with respect to properties

Sand is usually conditional before use.

Mulling machines are used to uniformly mull (mix thoroughly) sand with additives. Clay (bentonite) is used as a cohesive agent to bond sand particles (giving the sand strength). Zircon (ZrSiO4), Olivine (Mg2SiO4) and Iron silicate (Fe2SiO4) sands are often used in steel foundries for their low thermal expansion. Chromite (Fe2Cr2O4) is used for its high heat transfer properly.

Lecture-3

Molds

A mold is a container that has the cavity or cavities of the shape to be casted.

Flask: A flask is a wood or metal frame in which a mold is made. A flask is made of two principal parts, the cope (top section) and the drag (bottom section). To increase the depth of the cope and/or the drag, intermediate sections, known as cheeks, are used

Pouring basin or pouring cap: into which the molten metal is poured.

Sprue: through which the molten metal flows downward.

Runner system: channels to carry the molten metal from the sprue to the mold cavity. Gates are inlets into the mold cavity.

Risers: supply additional metal to the casting as it shrinks during solidification.

Cores: inserts made from sand. They are placed in the mold to form hollow regions or otherwise define the interior surface of the casting.

Cores are also used on the outside of the casting to form features such as telling on the side of a casting or deep external pockets.

Vents: carry off gases produced when the molten metal comes in contact with the sand in the molds and core. Also exhaust air from the mold cavity comes out through vents as the molten metal flows into the mold.

## Figure:

## Desirable characteristics of Molds

The mold must be strong enough to hold the weight of the metal.

The mold must resist the erosive action of the rapidly flowing molten metal during pouring.

The mold must generate a minimum amount of gas when filled with molten metal.

The mold must provide enough venting so that any gases formed can pass through the body of the mold itself, rather than penetrate the metal.

The mold must be refractory enough to withstand the high temperature of the molten metal and strip away cleanly from the casting after cooling.

The mold must permit the casting to contract after solidification.

## Classification of molds

Depending on the materials used, Molds are classified as follows:

Green-sand molds: Molds made with damp molding sand.

Skin-dried molds: Two methods..

First-The sand around the pattern to a depth of about ½ inch is mixed with a binder so that when it is dried it will leave a hard surface on the mold. The remainder of the mold is made up of ordinary green sand.

Second-The entire mold is made with green sand and then coat its surface with a spray or wash, which hardens when it is applied.

Spray used are: linseed oil, molasses water, gelatinized starch etc.

In both of them mold is dried either by air or by a torch to harden the surface and drive cut excess moisture.

Dry sand molds: Fairly coarse molding sand mixed with a binding material is used. Flasks are of metal, since molds must be oven baked before being used. It is free from gas troubles due to moisture. Skin-dried and dry-sand molds are widely used in steel foundries.

Loam molds: It is first built up with bricks or large iron parts; these parts are then plastered over with a thick Loam mortar, the shape of the cavity being obtained with sweeps or skeleton patterns. The mold is then allowed to dry thoroughly. It needs long time to make and is not used extensively.

Furan molds: Dry, sharp sand is thoroughly mulled with phosphoric acid which acts as an accelerator==> furan resin is added and mulling is continued==>the sand materials begins to air harden almost immediately.

CO2 molds: Clean sands is mixed with sodium silicate and the mixture is rammed about a pattern. When CO2 gas is pressure-fed into the mold, the sand mixture hardens. Very smooth and intricate castings are obtained. Used for core making.

Metal molds: these are used mainly in the die-casting of low-molting-temperature alloys. Accurate with smooth finish. Eliminate much machine work.

Special molds: Plastics, cement, plaster, paper, wood and rubber are all mold materials used to fit particular applications.

## Molding processes

Bench molding: is for small work, done on a bench of a height convenient to the molder.

Floor molding: When castings increase in size, with resultant difficulty in handling, the work is done on the foundry floor. This type of molding is used for practically all medium and large size castings.

Pit molding: Extremely large castings are frequently molded in a pit instead of a flask. The pit acts as the drag part of the flask and a separate cope is used above it. They sides of the pit are brick kind, and on the bottom there

Machine molding: Machines have been developed to do a number of operations that the molder ordinarily does by hand. Ramming the sand, rolling the mold, forming the gate and drawing the pattern can be done by these machines.

Mold preparation

For removable pattern:

The pattern is placed on a molding board.

The drag is placed on the board with pins down.

Molding sand is then riddled in to cover the pattern.

The sand is pressed around the pattern until the drag is completely filled.

The sand is firmly packed by the drag rammer.

After ramming the excess sand is leveled off with a straight bar called a strike rod.

Small vent holes are made through the sand to within a fraction of an inch of the pattern to insure the escape of gases.

The drag is then turned over so that the cope may be placed in position.

Before turning a little sand is sprinkled over the mold and a bottom board is placed on top. After rolling over the drag the molding board is removed exposing the pattern.

The surface of the sand is smoothed over with a trowel and covered with a fine coating of dry parting sand.

The cope is then placed on the drag, the pins on either side holding it in proper position.

To provide, a place for the iron to enter the mold, a tapered pin known as sprue pin is placed an inch to one side of the pattern.

The operations of filling, ramming, and venting the cope proceed in the same manner as in the drag.

The sprue pin is withdrawn, and funnel shaped opening is scooped out at the top so that there will be a fairly large opening in which to pour the metal.

The cope half of the flask is then carefully lifted off and set to one side.

Before the pattern is withdrawn, the sand around the edge of the pattern is usually moistened with a swab so that the edges of the mold hold firmly together when the pattern is withdrawn.

To loosen the pattern, a draw spike, is driven into it and rapped lightly in all directions.

The pattern is withdrawn by lifting the draw spike.

Before closing, a small passage, known as a gate must be cut between the cavity and the sprue opening.

Sometimes a hollow, known as riser is provided in the cope to supply hot metal as the casting cools and shrinks.

The mold surfaces may be sprayed, swabbed, or dusted with coating materials such as silica flour and graphite.

For disposable pattern:

The pattern, usually one piece, is placed on a board and the drag is molded in the conventional way.

Vent holes are added and the drag is turned over for molding the cope.

No parting sand is applied for the cope and drag will not be separated until the casting is removed.

The polystyrene pattern, including the gating and pouring system are left in the mold.

Molten metal is poured rather rapidly into the sprue, the polystyrene vaporizes and the metal fills the remaining cavity.

The mold is poured fast enough to prevent combustion of polystyrene, with the resulting carbonaceous residue. The gases due to vaporization of the material are driven out through the permeable sand and vent holes.

Figure:

Figure:

## Gating System

## The passage way for bringing the molten metal into the mold cavity. It includes: pouring basin, downgate or vertical passage known as a sprue, gate through which the metal flows from the sprue base to the mold cavity, a runner in large castings, which takes the metal from the sprue base and distributes it to several gate passage ways around the cavity.

## Characteristics of good gating system:

Metal should enter the cavity with as little turbulence as possible at or near the bottom of the mold cavity.

Erosion of the passageway or cavity surfaces should be avoided by properly regulating the flow of metal.

Metal should enter the cavity so as to provide, directional solidification if possible. The solidification should progress from the mold surfaces to the hottest metal so that there is always hot metal available to compensate for shrinkage.

Clay or other foreign particles should be prevented from entering the mold cavity.

Skimming gates may be used to trap slag or other light particles into the second sprue hole. The gate to the mold is restricted somewhat to allow time for the floating particles to rise into the skimmer.

Three types of gate are used in mold:

Parting gates

Top gates

Bottom gates

Top gate: Conductive to a favorable temperature gradient but	erosion may be high

Bottom gate: Offers smooth flow with a minimum of erosion but unfavorable temperature gradient.

Figure:

Riser: Risers are often provided in molds to feed molten metal into the main cavity to compensate for the shrinkage.

There are two types of riser

Open Riser: Top of the open riser in open, it is cylinder shape

Advantages: 	An open riser is easy to mold,

Air can be removed from it.

Disadvantages:	It is not placed in the drag.

More difficult to remove from the Casting.

Close/blind riser: Blind risers are domelike risers, found in the cope half of the flask, which are not the complete height of the cope.

Advantages: 	Can be placed at any position of the mold

Can be easily removed from the casting.

Disadvantages:	Difficult to mold

May draw liquid metal from solidifying casting.

Figure

## Chills:

Chills are metal inserts used to control solidification by carrying heat away from the solidifying metal at a rapid rate.

Chills are the metal shapes inserted in molds to speed up the solidification of a particular portion of the casting.

Chills equalize the cooling rate of thin and thick sections and thus prevents hot tears.

Chills promote progressive and directional solidification.

Types chills (I) External (II) Internal.

External Chills: It is rammed up in the mold walls. An external Chill is excellent for controlling cooling rates in critical region of castings.

Internal Chills: These are of same material as the molten metal. Thus are placed in the mold cavity before casting when molten metal enters into mold cavity, melts the block, which is used as internal chills, and prevents shrinkage void.

Feed here

External

Chill

Internal chill

## Patterns:

Used to mold the sand mixture into the shape of the casting.

## Patterns Materials:

Wood – for small production (white pine, mahogany, cherry etc.)

Metal – for high quality production

Brass

Cast iron

Aluminium

Plastics

Advantage of metal or plastic pattern:

Do not absorb moisture

Strong and dimensionally stable

Smooth surface finish.

Pattern material selection depends on

The size and shape of the casting

The dimensional accuracy

The quantity of castings required

The molding process to be used.

Strength and durability of the material selected for patterns must reflect the number of castings that the mold will produce.

Sometimes combination of materials is used to reduce wear in critical regions.

Patterns are usually coated with a partings agent to facilitate their removal from the molds.

Types of pattern

Solid or single piece pattern: generally used for simpler shapes and low quantity production. They are generally made of wood and are inexpensive.

Split pattern: many patterns cannot be made of a single piece because of the difficulty in molding. To eliminate the difficulty the patterns are made split, half rests in lower part and half in upper part.

Gated patterns: in production work where many castings are required, patterns are made of metal to give them strengths and to eliminate any warping tendency. The gates or runners for the molten metal are formed by connecting parts between the individual patterns.

Loose piece pattern: consists of loose pieces, which are necessary to facilitate withdrawing it from the mold.

Match plates: provide a substantial mounting for patterns. It consists of a flat metal or wooden plate to which the patterns and gate are permanently fastened.

Sweep pattern: they are used where the shape to be molded can be formed by the rotation of a curved line element about an axis:

## Rapid prototyping:

A recent development to mold and pattern making

For example, in investment casting wax patterns can now be replaced with accurate resin patterns by rapid prototyping.

In this case CAD data are used directly (without the need for dies) to make the pattern at a fraction of the time and cost of dies for making wax patterns.

Figures:

## Pattern allowances:

Shrinkage: metals shrink when they cool.

Cost iron 	– 	1/8 inch/foot

Brass 		-	3/16 inch/foot

Steel		-	¼ inch/foot			+ ve allowance.

Aluminium	-	5/32 inch/foot

and Magnesium

Draft: When a pattern is drawn from a mold, the tendency to tear away the edges of the mold in contact with the pattern is greatly decreased if the surfaces of the pattern are slightly tapered known as draft.

1/8 to ¼ in/foot (exterior)

¾  in/foot (interior)

Finish: positive allowance is provided for machining. For small and average-sized casting finish allowance is 1/8 inch.

Distortion: distortion allowance applies only to those castings of irregular shape which are distorted in the process of cooling because of metal shrinkage.

Shake: when a removable pattern is rapped in the mold before it is withdrawn, the cavity in the mold increases slightly. A shake allowance should be considered by making the pattern slightly smaller to compensate for the rapping of the mold.

Figure:

Lecture-5

## Cores

## Cores are utilized for castings with internal cavities or passages.

A core is a body, usually made of sand, used to produce a cavity in or on a casting.

Examples: forming the water jacket in a water cooled engine block and forming the air space between the cooling fins of an air cooled engine.

Cores are placed in the mold cavity before casting to form the interior surfaces of the casting.

figure:

Desirable properties:

Strength (green and dry)

Permeability

Ability to withstand heat or refractoriness

Collapsibility

Friability

A minimal tendency to generate gas

Core making

Core sand is placed in a core box. It can be blown into the box, rammed or packed by hand, or jolted into the box. The excess sand is struck off, and a drier plate is placed over the box. The core box is then inverted, vibrated or rapped, and drawn off the core. The core is then put in a core oven and backed.

## Core prints

Recesses that are added to the pattern to support the core and to provide vents for the escape of gases.

Core shifting: shifting of cores from its proper place is a major cause of defective castings.

Anchor: a core is subjected to an appreciable buoyant force when immersed in the liquid metal poured into the mold cavity.

Chaplets: serve to support cores that tend to sag or sink in inadequate core print seats. Chaplets also serve as anchor to keep the core in place during the casting process.

A chaplet is usually made of the same metal as, and becomes part of the casting.

Fig : Anchoring Cores with Chaplets.

Types of cores

Green sand core

Dry sand core

Green sand core

A green sand core is made of the same sand from which the mold has been made i.e. the molding sand.

Relatively cheap and popular.

Dry sand core

Dry sand core unlike green sand cores are not produced as a part of the mold.

Dry sand core is made separately and independent of the mold.

Backed sand or dry sand core has a binder that must be cured with heat.

Core making machines:

Cores of regular shapes and sections may be extruded and cut to length. A central vent hole is left by a wire extending from the center of the screw.

Figure:

Large cores are made by jolt-rollover, sand slinger and other machines.

Small and medium size irregular shape cores are usually made by hand. But if quantity is high, they are produced on a core blowing machine. This machine blows sand by compressed air through a core plate with holes arranged to pack the sand evenly and firming in the core box.

Core backing:

The cores that are bonded by oils must be baked for ultimate hardness and strength. The purpose of baking is to drive off moisture, oxidize the oil, and polymerize the binder.

A uniform temperature and controlled heating are necessary for baking an oil-bonded sand core. With linseed oil the temperature is raised at a moderate rate, and is held at about 200C for about 1 hr and then is allowed to fall slowly to room conditions.

Molding machines:

Serve: 	To pack sand firmly and uniformly into the mold.

To manipulate the flasks, mold, and pattern.

Three types of molding machines are:

Jolt-squeeze Molding Machine

Jolt-rollover Molding Machine

Sand slinger

Jolt-squeeze Molding Machines: A jolt-squeezer consists basically of a table actuated by two pistons in air cylinders, one inside the other. The mold on the table is jolted by the action of the inner piston that raises the table repeatedly and drops it down sharply on a bumper pad. Jilting packs the sand in the lower parts of the flask but not at the top. The larger cylinder pushes the table upward to squeeze the sand in the mold against the squeeze head at the top. A vibrator may be attached to the machine to loosen the pattern to remove it easily without damaging the mold.

Figure:

Jolt-rollover Pattern-draw Machines: A flask is set over a pattern on a table and is filled with sand and jolted. Excess sand is struck off, and a bottom board is clamped to the flask. The machine raises the mold and rolls it over onto a table or conveyor. The flask is freed from the machine. The pattern is vibrated, raised from the mold, and returned to loading position.

Figure:

The sand slinger: The sand slinger achieves a consistent packing and ramming effect by hurling sand into the mold at a high velocity. Sand from a hopper is fed by a belt to a high-speed impeller in the head. A common arrangement is to suspend the slinger with counter weights and move it about to direct the stream of sand advantageously into a mold. Sand slinger can be deliver large quantities of sand rapidly and are specially beneficial for ramming big molds.

Figure

Lecture-6

Casting defects:

Blow holes

Gas holes

Seam and plate

Misrum

Cold shut

Hot tear

Shrinkage Cavities.

Blow holes: Small holes visible on the surface of the casting are called open blows where as occurring below the surface of the casting.

Causes>>	 High moisture in sand resulting in low permeability, very hard ramming of sand and improper venting of mold.

Figure:

Gas holes: These are the holes appearing on the surface when it is machined or cut into sections.

Causes>>using faulty or poor quality metal, use excessive moist sand.

Seam and plate: - Seam is an impressed line on casting surface and plate is in the form of a layer of metal, partially separated from the main body of the casting section by scale (plate of hard material).

Causes>>Interrupted metal flow due to abrupt changes in casting section adn sharp section.

Figure:

Misrum:- It is a casting that is incomplete in its outermost sections, either long the to thickness is too large or because the metal was poured with insufficient superheat.

Causes>>	Too cold molten metal

Too thin casting section

Too small gates.

Cold shut: It is an interface within a casting that lacks complete fusion and is formed when two streams of liquid from two different directions come together after the leading surfaces are solidified.

Causes>>	Metal lacking in fluidity.

Too small gates

Too cold molten metal.

Figure:

Hot tear: Intergrannular (along grain boundaries) failure at a high temperature the larger sections for intensive strain induced by solid contraction of adjacent thinner section.

Causes>> 	Excessive mold hardness.

High drag and hot strength of sand mold.

Too much shrinkage of metal while solidifying.

Too low pouring temp.

Shrinkage Cavities: An internal void in a casting from the volume contraction that occurs during solidification. It causes for any casting.

#### Design consideration

(a)	Design for minimum casting stresses

(b)	Design for solidification

(c)	Design for metal flow

(d)	Cast mold design.

(e)	Design for minimum casting.

(f)	Functional design

Design rules:

External corner should be rounded with raddi that are 10% to 20% to section thickness. By rounding corners, the resistance of ductile metal to fatigue or static stress is increased.

In Joining section of unequal sizes the raddi plays an important role, A raddi of (a) 0.1 t the resistance to fatigue stress is united (b) 1t, there is 40 to 50% more stress endurance. (c) 4t, 120% more stress endurance than that with 0/1t radius.

Figure

Replace sharp angles and corners with suitable radii. When mold cavity is filled with molten metal the inside corner of the casting is heated to higher temp. Then other sections of mold cavity due to this over heating the metal at inside corners solidifies more slowly and this delay in solidification may cause shrinkage defects at this location.

Figure

Use tabular or cross-sections rather than standard I or H sections to obtain improved load bearing capabilities under complex load.